## Slide 1
Engineering Bacterial Nanocellulose Suspensions
Our expertise lies in tailoring nanofibril morphology, surface chemistry, and interparticle interactions to control suspension stability and rheological behaviour.

## Slide 2
Cellulose Nanocrystals CNCs
Morphology & surface characteristics
Length: 900 ± 300nm
Width: 25 ± 10 nm
Aspect ratio: 35- 40
ζ-potential: ≈ −34.07 ± 1.25 mV
Mobility (µm·cm/V·s): −2.670 ± 0.097 µm·cm/V·s
Sulfate group content = 218.3 ± 2.1 µmol g⁻¹
Isotropic to ordered Liquid Crystalline Phase

## Slide 4
Cellulose nanofibrils CNFs
Morphology & surface characteristics Length: >50 µm, extending beyond the SEM field of view Width: 86.4 ± 40.8 nm Aspect ratio: >580 ζ-potential: ≈ 0 mV Surface: Non-functionalised CNFs
Stable suspension with no phase suspension
Long, highly entangled CNFs can remain physically stable through network formation even without strong electrostatic stabilization.

## Slide 5
Cellulose nanofibrils CNFs
Morphology & surface characteristics Length: 5.46 ± 1.21 µm Width: 30.3 ± 19.2 nm Aspect ratio: 180 ζ-potential: ≈ -7 mV Surface: functionalised CNFs

## Slide 6
1.73 ± 0.32 µm
Morphology & surface characteristics Length: Width: 24.7 ± 12.8 nm. Aspect ratio: 70 ζ-potential: ≈ −23.0 ± 0.4 mV Surface: functionalised CNFs
Cellulose nanofibrils CNFs

## Slide 7
Nanofibrils with varying aspect ratios and network behavior
CNFs
CNCs

## Slide 8
Nanofibrils with varying aspect ratios and network behavior
CNF_LA_1_2
CNF_LA_1_9
CNF_OA